Experimental setup

### Sample
Titanium implant physical size	3.5mm (diameter), 8mm (length); / 2.5mm newly formed bone, 5.5mm recipient bone
Acrylic cylinder	(6.5 x 6.5 x 6.5) mm

### Physical Setup
(Source–Sample–Detector) distances	Source–Sample: ~145m; / Sample–Detector: ~1-20m (± 1m precision);
Exposure time	100’s of ns to ms range
Number of projections (0-360°)	1999 equiangularly spaced

### Source
Source dimension	~ 0.1 mm
Current	~ 0-300 mA
Voltage	67 keV (Pinholt), 50 keV (our article), range for ID19 is 6-120 keV, other places say 50-280 keV, yet again 10-150 keV
Beam size	Minimum (H x V): 2.8 x 1.4 mm² / Maximum (H x V): 320.0 x 17.0 mm²
Spot size on sample	0.1-30mm (horizontal); 0.1-10mm (vertical);

### Image
Voxel size	1.875 µm (range 0.4-40 µm)
ROI voxels	~ (3500 x 3500 x 3500)

### Densities
Titanium (Ti)	4.53 g/cm³
Blood (H, O, N, C, Fe)	1.06 g/cm³
Bone (mainly Ca, P, Mg, S)	0.9-1.4 g/cm³
Resin (standard resin for 3D-print)	1.11 g/cm³
Air	1.3·10⁻³ g/cm³

### References
- Our article
- ESRF webpages on ID19 beamline
- Application of high resolution synchrotron micro-CT radiation in dental implant osseointegration, Neldam et al.